M O D E L L I N G  B A N D A G E S

Modelling and reinforcement fabric for industry and handicraft applications

A fabric coated with synthetic hard gypsum

- for industrial mould applications to produce transportable models (e.g. laminates in car, airplane and ship model construction)

- to sheath insulated lines

- for modelling in studios

- for do-it-yourselfers, e.g. for model railway construction and relief design

Special advantages

-	Can be used instead of synthetic resins

- Simple processing

- Good physiological tolerability

- Problem-free disposal

Characteristics:

Coated fabric

Gypsum coating weight per unit area
	approx. 410 g/m²

Immersion time	approx. 5 sec

Solidification time	approx. 3 min

Special notes

MODELLING BANDAGES T can be effectively combined in industrial mould construction with the mould mass LUDUR 500 M.

Processing:

Immerse modelling bandages for approx. 5 seconds in water, squeeze out briefly, apply immediately to the desired surface, press on lightly and smooth.

Each third or fourth layer can be applied in a dry state. A wallpaper roller is well-suited for smoothing.

For smaller models, 3-5 layers are sufficient, with an increasing size of the models, the number of layers is to be increased to obtain a good stability.

For processing with LUDUR 500 M please read the special data sheets!

Delivery sizes

length 2 m, width 10 cm, film-packaged

length 3 m, width 6 cm, film-packaged

length 3 m, width 8 cm, film-packaged

length 3 m, width 10 cm, film-packaged

length 3 m, width 15 cm, film-packaged

length 3 m, width 20 cm, film-packaged

Storage life

At least 1 year from production in well-closed, humidity-tight drums and given dry storage.

The above information is given to our best knowledge and after thorough examination. We guarantee perfect quality of our products, however, shall not be liable for further processing results which are normally beyond our control.